## Slide 1: Nucleation
Peter W. Voorhees
Department of Materials Science and Engineering
Northwestern University
Evanston, IL

## Slide 2: Outline
Equilibrium description of clusters
Dynamics of reversible nucleation
Irreversible nucleation
Island coarsening

## Slide 3: References
A. Pimpinelli and J. Villian, Physics of Crystal Growth, Cambridge 1998.
P. Noziéres, Shape and Growth of Crystals, in Solids Far from Equilibrium, Ed. C. Goodrèche, Cambridge 1992.
J.W. Evans, P. A. Thiel, and M.C. Bartelt. Morphological evolution during epitaxial thin film growth: Formation of 2D islands and 3D mounds. Surface Science Reports 61, no. 1-2 (2006): 1-128.

## Slide 4: The Early Stages of Epitaxy: Submonolayer
Equilibrium: F=0

## Slide 5: Equilibrium Phase Diagram
G
I
is the number of lattice sites on the surface

## Slide 6: Equilibrium: Assumptions
Isotropic edge energy
Islands are stress free
F = 0
Dilute concentration of islands
Isothermal

## Slide 7: Equilibrium between a cluster and the gas
where
And P is an energy per unit area

## Slide 8: Edge energy and Edge stress
For a circular cluster:
Force balance:
Force acting along a line:
Force due the stress at the edge:
R
f
f
Thus,
In a crystal stress can be of either sign, and not equal to the edge energy

## Slide 9: Reversible Nucleation: Assumptions
Isotropic edge energy
Islands are stress free
F = 0
Dilute concentration of islands
Isothermal

## Slide 10: Energy of Nucleation
The critical nucleus is that cluster that is in unstable equilibrium with the adatom gas
E
X
Metastable
Stable
Unstable
Equilibrium is given by an extremum in the energy
Thus, the equilibrium conditions describe the conditions for the critical nucleus

## Slide 11: Reversible Work for the Formation of the Critical Nucleus
The cluster sits in a very large adatom sea
Thus, the cluster is formed under conditions of constant,
Note: pressure (energy/area) is not constant
Thus, the reversible work of the critical nucleus is,
Initial
Final

## Slide 12: Reversible Work for the Formation of the Critical Nucleus
Initial
Final
Thus,
At equilibrium,
Thus, the first term is negative

## Slide 13: Reversible Work for the Formation of the Critical Nucleus
The reversible work is:
Since > 0, , and thus fluctuations are required to create a nucleus
If the nucleus is incompressible, and by considering the pressure dependence of
The critical radius is

## Slide 14: Anisotropic Step Free Energy
Step energies can be anisotropic,
STM images (25 Å~ 25 nm2) of 0.1 ML Ag/Ag(100)
[01]
[10]
If is analytic, then
Type equation here.

## Slide 15: Anisotropic Step Free Energy
The critical nucleus is in equilibrium
Assume is analytic, then
Where the stiffness of the step free energy is

## Slide 16: Anisotropic Step Free Energy
The shape of the nucleus is given by the Wulff shape, which is the shape that satisfies
For a given Wulff shape the reversible work for the formation of the critical nucleus is
where the the area and perimeter depend on the Wulff shape

## Slide 17: Highly Anisotropic Step Free Energy
In this case, for certain orientations
This leads to facets, or flat edges
Curvature still exists!
For example, for a square Wulff shape, equal step free energy along ,
The same procedure holds
[01]
[10]

## Slide 18: The Effects of Stress
Stress is common in heteroepitaxy, and can be very large
In this case,
For a review: Voorhees, Peter W., and William C. Johnson. "The thermodynamics of elastically stressed crystals." Solid State Physics-Advances in Research and Applications (2004): 1-201.

## Slide 19: Kinetics of Reversible Nucleation
Need to define the work of formation for a cluster that is not in equilibrium,
R
0
0

## Slide 20: Kinetics of Reversible Nucleation
In the single-phase region
R
0
0
1
Equilibrium Distribution of Clusters
( number of clusters of size per area)

## Slide 21: Master Equation
The number of clusters with i atoms per area changes by the addition or removal of an atom (dilute solution of clusters)
The current is
-
Need expressions for the probabilities W
for i where is the nonequilibrium density of clusters

## Slide 22: Master Equation
Key assumption: the impingement and emission rates are related
We assume a detailed balance. At equilibrium the currents are zero
Thus, the emission rate is,
The emission rate is always nonzero (not true in all cases), and the rate is related to the equilibrium distribution of clusters
-
=

## Slide 23: Master Equation
The impingement rate depends on the process setting the growth of a cluster
If the cluster growth is diffusion limited, then follows from the flux of adatoms into a cluster of size n
If the growth is limited by attachment at the step edge (isotropic kinetics)

## Slide 24: Master Equation
The number of clusters with n atoms per area changes by the addition or removal of an atom (dilute solution of clusters)
Given an initial distribution for clusters, this is a set of ODE’s for the evolution of the cluster size distribution
Straightforward to solve for large systems
Can we make any progress analytically?
for i

## Slide 25: Fokker-Planck or Zeldovitch Equation
Assuming detailed balance the current is
or
Assume to be much larger than one, expand in a Talyor’s series about to first order,

## Slide 26: Fokker-Planck or Zeldovitch Equation
We need to connect the current to the change in cluster size distribution
Assume that a cluster flows from one size to another smoothly, i.e. no coalescence
Since

## Slide 27: Fokker-Planck or Zeldovitch Equation
This yields the Fokker-Planck or Zeldovitch equation
Substituting the equilibrium distribution of clusters,
Diffusion term accounts for clusters random walking to subcritical sizes
0
0
Diffusion
Drift

## Slide 28: Solving the Fokker-Planck Equation
Steady state nucleation,
The current is not zero since the boundary conditions are
Again, assuming a dilute concentration of clusters

## Slide 29: Solving the Fokker-Planck Equation
Thus, we need to solve,
With
Employing the approximation,

## Slide 30: Steady State Nucleation
This yields the steady state nucleation current
where is the Zeldovitch factor,
and

## Slide 31: Steady State Nucleation: Observations
The Zeldovitch factor is It accounts for clusters flowing backwards across
The major factor controlling the is the exponential term. Since the value of the nucleation current is extremely sensitive to changes in the step free energy
0
0
kT
2/Z

## Slide 32: What Happens if the Adatom Supersaturation is Large?
The critical radius is,
So, as increases, or, (a single atom)
The emission rate is very small compared to the impingement rate, detailed balance no longer holds
Conclusion: the nucleation process is entirely kinetically controlled

## Slide 33: Irreversible Nucleation
Isotropic diffusion on unreconstructed substrates
After landing on the substrate atoms diffuse by surface diffusion, D
Growth occurs by diffusion-limited aggregation
Stable islands are immobile
Diffusion rate along a step determines is fast, thus islands assume the Wulff shape
No adatom emission from an island
No evaporation from substrate, removal of atoms by step edges and other defects

## Slide 34: Deposition and Diffusion
Atoms hop along the substrate at a rate
The surface diffusion coefficient is for a surface with four-fold symmetry
Deposition rate is in monolayers/sec
The ratio, is a control parameter measuring rate of growth compared to the rate of diffusion

## Slide 35: Island Morphology
The morphology of island is a function of deposition temperature and the rate of diffusion along a step
Pt Islands on Pt (111) fixed deposition rate
300K
400K
500K
600K
T. Michely, J. Krug, Islands, Mounds, and Atoms, 2004.

## Slide 36: Rate Equations for Island Growth
Similar in spirit to the master equations for nucleation, but related entirely to the dynamics of atom motion
The rate of a cluster growth is
where is the capture number to cluster, measures the direct capture of deposited atoms on islands
For compact islands, or the area of the island

## Slide 37: Rate Equations for Island Growth
For adatoms,
As in the reversible nucleation problem, the physics of growth are contained in the capture numbers
We shall employ a mean-field approach to defining the capture numbers, see Bales and Chrzan, 1994. A similar approach can also be used to study the coarsening of islands.
=

## Slide 38: Capture Numbers
Consider an island of radius embedded in an ensemble average system of islands and monomers.
Assuming no barrier to incorporation of adatoms at the step edge, and irreversible attachment. Thus,
and

## Slide 39: Capture Numbers
The mean field equation for the diffusion of adatoms must agree with that from rate theory thus,
is the screening distance, or a distance a monomer travels before being captured by an island or another monomer
is the fraction of the flux that lands on a bare substrate

## Slide 40: Capture Numbers
To solve this, employ the quasistationary approximation where the growth rate of the particle is slow compared to diffusion
The diffusion field is given by a solution to
However, this never holds for all
Thus, neglect deviations in the atom concentration from the average, Subtracting the two equations,

## Slide 41: Capture Numbers
Solution is
Since
Thus

## Slide 42: Irreversible Nucleation
Thus, using these capture numbers, we solve
and
(One needs to be careful about )

## Slide 43: Comparison to Kinetic Monte Carlo Simulations
KMC
Rate
(a) D/F = 105, (b) D/F = 107, (c) D/F = 109

## Slide 44: Scaling Laws
Neglect direct impingement,
Sum defining the coverage , and the total number of clusters,

## Slide 45: Scaling Laws
For the number of adatoms
Neglecting compared to , and

## Slide 46: Scaling Laws
For the average cluster size, using the two rate equations
Along with
we can deduce scaling relations that are consistent with these equations
Notes: <sigma>* a slightly different definition of average

## Slide 47: Scaling Laws
Neglecting the logarithmic dependence of on

## Slide 48: Irreversible Nucleation: Extensions
Isotropic diffusion on unreconstructed substrates
After landing on the substrate atoms diffuse by surface diffusion, D
Growth occurs by diffusion-limited aggregation
Stable islands are immobile
Diffusion rate along a step determines is fast, thus islands assume the Wulff shape
No adatom emission from an island
No evaporation from substrate, removal of atoms by step edges and other defects
See Pimpinelli, Jensen, Larralde, Peyle, Directions Condensed Matter Phys. Vol. 14
F has units of atoms/(site time)

## Slide 49: Coarsening
Consider the limit where is small
Thus, emission is possible and local equilibrium is present at the island-adatom gas interface
Thus, for circular islands
Since the chemical potentials are functions of the pressure, and

## Slide 50: Gibbs-Thomson Equation
For small changes in adatom concentration from that at a planar step edge,
Where is the capillary length, is a function of and free energy of the gas phase.

## Slide 51
Coarsening
concentration
distance

## Slide 52: Coarsening
constant
magnification

## Slide 53
SELF SIMILARITY
magnification
scaled by the
average particle
size
constant
magnification
Hardy, Voorhees, 1988

## Slide 54: Diffusion-limited Coarsening
Mean field approach accounting for the flow of adatoms from one cluster to another
The flux into or out of an island,
J.A. Marqusee, J.Chem. Phys, 1984
The source and the sink terms must balance since there is no flux
Solve the equation in the quasistationary approximation

## Slide 55: Diffusion-limited Coarsening
Giving
Thus,
The screening length is a function of the island size distribution,

## Slide 56: Diffusion Limited Coarsening
The island size distribution evolves by the continuity equation
Adatom conservation,
Seek a scaling or similarity solution

## Slide 57: Diffusion Limited Coarsening
With the results,
Unique island size distribution when the particles are scaled by
The shape of the distribution depends on

## Slide 58: Attachment limited Coarsening
Since there is no long-range diffusion the growth rate is given by
A similar analysis shows,